bmcs group
Projects / Software Package Structure
Local evaluation of energy dissipation → fracture energy
Rostislav Chudoba
Institute of Structural Concrete

---
topics

---
Structure of repos and packages in the bmcs-group
Data Processing
High-Cycle-Fatigue-Data	high-cycle-fatigue-tool	@hs
Respose Surface Ironing	rs_iron	@jb
Crack detection tool	dic_cdt	@vs
Semianalytical models
Probabilistic multiple-cracking model	bmcs_fragmentation	@hs
Shear zone	bmcs_shear_zone	@fs
Reinforced beam response	bmcs_beam	@sr
Numerical models
Material model development	bmcs_matmod	@ab @mar
Nonlinear finite element simulator	bmcs_nlfes	@rc @ab
Folding process	oricreate	@rc
Discrete particle latice model	dplm	@rch @mar
[Speaker Notes: Scale up in size compared to small scale studies. The size was 3 m times 2,14 m. The crease pattern and the final form werde determined by geometric considerations. Note: this is only for simple cases possible Concept for folding: Steel ropes placed underneath the fabric along the crease lines  lifting Folding with scaffolding and gravitational force. Within the final configuration the creases were fixed with grout. No movement possible anymore. Alternative approach for folding with another barrel vault]

---
Specialized model applications – hierarchy
Bar – uniaxial tension
Pull-out	analytical / numerical
Crack bridge	analytical / numerical
Tensile test	analytical
Reinforced beam
Moment-curvature	CS designer
Reinforced beam deflection – SLS design
Beam stability analysis
Reinforced beam
Shear zone - discrete crack
RC beam simulator
[Speaker Notes: Scale up in size compared to small scale studies. The size was 3 m times 2,14 m. The crease pattern and the final form werde determined by geometric considerations. Note: this is only for simple cases possible Concept for folding: Steel ropes placed underneath the fabric along the crease lines  lifting Folding with scaffolding and gravitational force. Within the final configuration the creases were fixed with grout. No movement possible anymore. Alternative approach for folding with another barrel vault]

---
Numerical standalone model applications
Matetial model demonstrators
Slide model	monotonic / cyclic / fatigue
Microplane model	monotonic / cyclic / fatigue
Test simulators (matmod + nlfes)
Compression test
Pull-out Test
Notched cylinder shear test
Beam – combined bending / tension compression
[Speaker Notes: Scale up in size compared to small scale studies. The size was 3 m times 2,14 m. The crease pattern and the final form werde determined by geometric considerations. Note: this is only for simple cases possible Concept for folding: Steel ropes placed underneath the fabric along the crease lines  lifting Folding with scaffolding and gravitational force. Within the final configuration the creases were fixed with grout. No movement possible anymore. Alternative approach for folding with another barrel vault]

---
This is really useful! We can evaluate dissipated energy locally!
If we know where the localization and crack propagation occurs,
we can focus just onto this region and ignore the non-dissipative (elastic/unloading) rest of the domain
→ this is the fundamental concept behind methods describing fracture
\color{white} G = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x

---
How to evaluate energy dissipation?
ideal plasticity
G(t) = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x

---
How to evaluate energy dissipation?
ideal plasticity
G(t) = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x = \int_0^w P(w) \, \mathrm{d}w - \int_{\Omega_\mathrm{el}} E \varepsilon(x) \varepsilon(x) \, \mathrm{d}x
W = \int_0^{w} P(w) \, \mathrm{d} {w}
U_\omega = \frac{1}{2} P w
U_\pi = \frac{P^2}{2K_0}
G = W - U
U = \int_{\Omega_\mathrm{el}} \sigma(x) \varepsilon(x) \, \mathrm{d}x
G = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x

---
How to evaluate energy dissipation?
ideal plasticity
this only holds for
a bond-slip law with
constant stress
W = \int_0^{w} P(w) \, \mathrm{d} {w}
U_\omega = \frac{1}{2} P w
U_\pi = \frac{P^2}{2K_0}
G = W - U
U = \int_{\Omega_\mathrm{el}} \sigma(x) \varepsilon(x) \, \mathrm{d}x
G = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x
G(t) = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x = \int_0^w P(w) \, \mathrm{d}w - \int_{\Omega_\mathrm{el}} E \varepsilon(x) \varepsilon(x) \, \mathrm{d}x

---
How to evaluate energy dissipation – for softening materials?
ideal plasticity
for a general bond-slip law we have to take a time
integral of a energy release rate
G(t) = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x = \int_0^w P(w) \, \mathrm{d}w - \int_{\Omega_\mathrm{el}} E \varepsilon(x) \varepsilon(x) \, \mathrm{d}x
W = \int_0^{w} P(w) \, \mathrm{d} {w}
U_\omega = \frac{1}{2} P w
U_\pi = \frac{P^2}{2K_0}
G = W - U
U = \int_{\Omega_\mathrm{el}} \sigma(x) \varepsilon(x) \, \mathrm{d}x
G = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x
\tau \; [\mathrm{MPa}]
s \; [\mathrm{mm}]

---
How to evaluate energy dissipation – for softening materials?
ideal plasticity
softening/hardening plasticity
damage
(see thermodynamics)
G(t) = \int_0^t \int_{\Omega_\mathrm{diss}} \tau \dot{s}_\mathrm{pl} \, \mathrm{d}x \; \mathrm{d}\theta
G(t) = \int_0^t \int_{\Omega_\mathrm{diss}} Y \dot{\omega}_\mathrm{pl} \, \mathrm{d}x \; \mathrm{d}\theta
G(t) = \int_{\Omega_\mathrm{diss}} \tau(s,x) s(x) \, \mathrm{d}x = \int_0^w P(w) \, \mathrm{d}w - \int_{\Omega_\mathrm{el}} E \varepsilon(x) \varepsilon(x) \, \mathrm{d}x
W = \int_0^{w} P(w) \, \mathrm{d} {w}
U_\omega = \frac{1}{2} P w
U_\pi = \frac{P^2}{2K_0}
G = W - U
U = \int_{\Omega_\mathrm{el}} \sigma(x) \varepsilon(x) \, \mathrm{d}x
G = \int_{0}^{t} \int_{\Omega_\mathrm{diss}} \tau(s,x) \dot{s}(x) \, \mathrm{d}x \, \mathrm{d}t
\tau \; [\mathrm{MPa}]
s \; [\mathrm{mm}]

---
Fundamental idea behind the fracture energy
softening material behavior
localization strains into a discontinuity
energy dissipation can be related to a localized crack

---
Consequences of softening behavior

---
Why Is it important to evaluate energy dissipation → fracture energy?
The fact that energy dissipates locally
leads to the idea that it is independent
on the size and on boundary conditions
→ objective material property
A
P\;[\mathrm{N}]
w\;[\mathrm{m}]

---
Example
Consider a bond-slip law
with softening
\tau \; [\mathrm{MPa}]
s \; [\mathrm{mm}]
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)

---
Example
Consider a bond-slip law
with softening
\tau \; [\mathrm{MPa}]
s \; [\mathrm{mm}]
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}

---
Example
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}

---
Example
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}

---
Example
Observation: constant rate of energy dissipation
→ stable process, independent on BC
→ objectivity → material characteristics
Energy dissipated per unit area?
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}

---
Example
Observation: constant rate of energy dissipation
→ stable process, independent on BC
→ objectivity → material characteristics
Energy dissipated per unit area?
?
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}
A_\mathrm{F} = 50000 \; \mathrm{mm}^2
G_{t=1} = 21000\;\mathrm{Nmm} \implies G_{\mathrm{F}} = 21000 / 50000 = 0.41\;\mathrm{N/mm}

---
Conclusion – how to determine fracture energy?
1 – Run a test
2 – Evaluate the area below the P(w) curve
3 – Subtract stored energy
4 – Divide by the total debonded interface area
?
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}
A_\mathrm{F} = 50000 \; \mathrm{mm}^2
G_{t=1} = 21000\;\mathrm{Nmm} \implies G_{\mathrm{F}} = 21000 / 50000 = 0.41\;\mathrm{N/mm}

---
How to predict the total dissipated energy without simulation?
Regarding the softening bond-slip law
→ We don’t need to know
Q: Does the total dissipated energy change for d = 4mm?
G_\mathrm{F} = \int_{0}^\infty \tau(s) \, \mathrm{d} s = \frac{1}{2} \cdot 10 \cdot 0.1 = 0.5 \; \mathrm{N/mm}
\tau \; [\mathrm{MPa}]
s \; [\mathrm{mm}]
G_\mathrm{total} = G_\mathrm{F} A_\mathrm{F} = 25000\;\mathrm{Nmm} = 25 \; \mathrm{J}
\color{blue} P(w), \varepsilon(x), \sigma(x), , s(x), \tau(x), \ldots
500 \; \mathrm{mm}
100 \; \mathrm{mm}
P(w)
E_\mathrm{m} = 28000 \; \mathrm{MPa}
E_\mathrm{f} = 240000 \; \mathrm{MPa}
d = 3\;\mathrm{mm}
A_\mathrm{F} = 50000 \; \mathrm{mm}^2

---
Consequences?
No volume integrals necessary, no state variables necessary
To obtain the fracture energy we need
a test with a clearly observable discontinuity
of a known area
The test should ideally
reach zero level of
Then
G_\mathrm{F}
G_\mathrm{F} = G_\mathrm{total} / A_\mathrm{F}
G(t) = \int_0^t \int_{\Omega_\mathrm{diss}} \tau \dot{s}_\mathrm{pl} \, \mathrm{d}x \; \mathrm{d}\theta = \int_0^w P(w) \, \mathrm{d}w - \int_{\Omega_\mathrm{el}} E \varepsilon(x) \varepsilon(x) \, \mathrm{d}x
A_\mathrm{F}
P\;[\mathrm{N}]
w\;[\mathrm{m}]
G_\mathrm{total}
P

---
Fracture energy of concrete cracking
G_\mathrm{F}
P(u)\;\;[\mathrm{mm}]

---
Fracture energy of concrete cracking
G_\mathrm{F}
\dot{\omega}, \dot{w}_\mathrm{pl}
P(u)\;\;[\mathrm{mm}]
\sigma \; [\mathrm{MPa}]
w \; [\mathrm{mm}]
G_\mathrm{F}
f_\mathrm{t}

---
Fracture energy of concrete cracking
G_\mathrm{F}
\dot{\omega}, \dot{w}_\mathrm{pl}
P(u)\;\;[\mathrm{mm}]
P\;[\mathrm{N}]
u\;[\mathrm{mm}]
G_\mathrm{total}
W(u_{\max})
\sigma \; [\mathrm{MPa}]
w \; [\mathrm{mm}]
G_\mathrm{F}
f_\mathrm{t}

---
Usage of fracture energy
Calibrate the softening branch of
a cohesive crack model – the measure
of ductility of quasi-brittleness of the material
By calibrating the softening law
from the curve of a beam with depth
we can predict the curve of a beam with depth
Softening law can be transformed to damage function
and applied in finite element simulations
\sigma \; [\mathrm{MPa}]
w \; [\mathrm{mm}]
G_\mathrm{F}
P(u)
P(u)
H_1
H_2
f(w)
\omega(\varepsilon)
f_\mathrm{t}

---
Usage of fracture energy – outlook
Regularize finite-element models
of concrete cracking to deliver mesh
independent results
\sigma \; [\mathrm{MPa}]
\varepsilon \; [\mathrm{-}]
G_\mathrm{F}

---
Possible tasks
Given a measured force-displacement curve from pull-out
or from a bending test derive the fracture energy characterizing
the localization process of the interface or concrete matrix
Given a material strength and fracture energy, derive a
bond-slip law or crack opening law
Exercise: X0601 – Energy supply and dissipated energy
\sigma(w)
\tau(s)